# 3001-068

## Technical Data

Product Description – A medium tack masking tape for use in interior applications. The product consists of a low density polyethylene backing, coated with a custom formulated water based acrylic adhesive.

# Product Characteristics

## Construction

Backing			Clear, white and blue low density polyethylene 		Adhesive			water based acrylic

Total Thickness 		3.0 nominal

## Performance

Tensile Strength (psi)					Test Method

MD			3800			ASTM D 882

TD			3000			ASTM D 882

Elongation (%)

MD			470			ASTM D 882

TD			950			ASTM D 882

Adhesion to steel  (oz/in)	5.0 – 9.0  		PSTC - 101

## The physical properties listed above are typical values and are not to be considered as specifications. Our suggestions for use are based on tests we believe to be reliable. However, the purchaser must determine the suitability of the product for their internal use.  Main Tape assumes no liability for claims beyond those outlined within our Limited Warranty, which includes replacement value of Main Tape product proven defective. For full disclosure of the Limited Warranty, please contact your Main Tape representative.

### Typical Uses -  Ideal for the masking and protection of stainless steel with a #3 or #4 finish and matte anodized and mill finish aluminum. Excellent performance on matte painted metals and matte and textured  high pressure laminates. Adequate performance on nameplate substrates such as textured PET and polycarbonate.

# Text boxes

#### MAIN TAPE COMPANY

One Capital Drive, Suite 101, BLDG. 1, Cranbury, New Jersey  08512